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Synthetic Film
(HS Code: 3920102500, 3920108900, 3920202100)
Biaxially Oriented Polypropylene Film 

(BOPP Film)
Biaxially oriented polypropylene film is used for packing of food products, medical products, perfume and cosmetics, light industry and household articles, tobacco products; for printing; for manufacturing of metalized and multilayer films, composite materials and consumer goods.

Depending on application and used feedstock we can produce the film grades as follows:

BOPP П1, П2 - transparent film without heat sealable layers, designed for packing of food products, paper and cardboard gloss lamination, self-adhesive film materials manufacturing;

BOPP С – transparent heat sealing film designed for packing of food products, medical products, perfume and cosmetics, light industry and household articles; multilayer films manufacturing. It is used at semi-automatic and automatic machines of low and medium capacity;

BOPP У -packing film, designed for packing of food products and household goods.
	Parameter description
	Standard value

	Form of manufacture
	Roll

	Film shape
	web

	Film grade
	BOPP П1
	BOPP П2
	BOPP С
	BOPP У

	Film thickness, mm
	0,015-0,060
	0,015-0,060
	0,015-0,060
	0,015-0,060

	Nominal width, mm
	100-1640

	Roll diameter, mm
	≤450 mm for film width of 100-350 mm; ≤600 mm for film width of 351-1640 mm

	Inner diameter of tube , mm
	76 or 152

	Shelf life
	12 months from the date of manufacture; 3 months from the date of manufacture for BOPP СМ and BOPP СП films

	Storage conditions
	Indoor storage at temperature +5 °С - + 40 °С, avoid direct sunlight

	Packing type
	Palletized unit loads
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Coextruded Polyethylene Film
Coextruded polyethylene film is used for packing of food products, light industry and household articles, household chemicals, hygienic and sanitary products, products for industrial and technical application. Also the film can be used for manufacturing of multilayer metalized films and consumer goods (bags, parcels); individual and multiple packing and palletizing of the goods; in agricultural industry for cladding plant cultivation facilities (greenhouses, hothouses),and for packing, preservation and storage of grassy animal feed.

We produce the following types of coextruded polyethylene film:

CPE-У - dyed or undyed film designed for packing of food products, detergents, soil, peat and fertilizers, polymer pellets; it can be used in agricultural industry for cladding plant cultivation facilities (greenhouses, hothouses);it also can be used for laminated films manufacturing. It is used for manual and automated packing of any capacity.

CPE-dairy - white (black & white) film with either white outer and inner layers or white outer layer and black inner layer. The film is designed for packing of dairy products and also can be used for packing of other food and nonfood products. It is used at automatic and semi-automatic machines of low and medium capacity.

Grade СPE-T –dyed and undyed thermosetting film designed for packing of food products, multiple packing and palletizing of the goods consisting of individual items (household articles, wallpaper, office supplies, newspapers, magazines, books) including the goods in consumer containers (cases, boxes, bottles, sacks, cans, etc). It is used at automatic and semi-automatic machines of low and medium capacity.

CPE-stretch–standard-plus – undyed film designed for individual and multiple packing and palletizing of the various goods (food products, beverages, packing materials, furniture, etc.). It is used at automatic pallet wrapping machines of high capacity.

CPE-agro stretch – dyed film for packing, preservation and storage of grassy animal feed, ground or unground, in a form of compacted rolls with moisture content of 40 % to 55 %.
	Parameter description
	Standard value

	Form of manufacture
	roll

	Film type
	Sleeve, half-sleeve, web

	Film grade
	CPE-У
	CPE-dairy
	CPE-Т
	CPE-stretch-standard-plus
	CPE-agro stretch

	Film thickness, mm
	0,020-0,200
	0,060-0,150
	0,020-0,150
	0,020-0,040
	0,025

	Film width, mm
	200-1600
	200-1600
	200-1600
	350-1400
	500 или 750

	Roll diameter, mm
	≤ 700

	Inner diameter of tube, mm
	76 or 152

	Shelf life
	36 months from the date of manufacture;
12 months from the date of manufacture for food-grade films, CPE-stretch-standard, CPE-stretch-standard-plus and CPE-agro stretch films;
6 months for CPE-M grade films.

	Storage conditions
	Indoor storage at temperature -50 oС to + 40 oС, avoid direct sunlight; for CPE-stretch-standard, CPE-stretch-standard-plus and CPE-agro stretch films storage temperature shall be +5 oС - + 40 oС.

	Packing type
	- wrapping in one-layer polymer film fixed at the ends of a roll (primary packing) or putting into boxes made of corrugated cardboard (for CPE-agro stretch);
- primary packing on the pallets (except for CPE-agro stretch films);
- palletized unit loads


	Thermosetting Polyolefine Films (POF Films)
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Thermosetting polyolefine film is used for packing of food products (bakery and confectionery products, tea, semi-finished products, fast food products, deep-frozen products, fruit and vegetables, meat, fish, poultry, seafood, etc.), as well as for packing of toys, cosmetics, various printed articles (newspapers, magazines, CD/DVD), finishing materials (wallpaper, wall panels, ceiling panels, etc.), office supplies, household articles, articles for industrial and technical application, for packing of light industry and household articles and consumer goods.

The film is used at manual, semi-automatic and automatic thermosetting packing machines.


	

	Parameter description
	Standard value

	Form of manufacture
	Roll

	Film shape
	web
	half sleeve

	Film thickness, mm
	0,0125-0,0250

	Film width, mm
	350-1500
	200-850

	Roll diameter, mm
	≤ 350

	Internal diameter of tube, mm
	76

	Shelf life
	36 months from the date of production

	Storage conditions
	Indoor storage at temperature -30 °С to + 35 °С, avoid direct sunlight

	Packing type
	Boxes made of corrugated cardboard; palletized unit loads


We have our own logistics department and can sell products on FCA, DAP and DDP basis.
tel. +375 222 49 99 39, 49 95 82; fax: +375 222 76 40 11, 76 40 12
e-mail: market@khimvolokno.by                                                                               www.khimvolokno.by

[image: image5.wmf] 

_1489482538.doc



