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Polyester Staple Fiber (100% Virgin)
(DMT base)
(HS Code 5503200000)
Physical and mechanical properties

	№
	Nominal linear density, tex
	Description
	Application
	Specific breaking load, mN/tex, not less than
	Elongation at break, %, not more than
	Number of crimps per 1 cm
	Linear shrinkage in boiling water, % not more than

	1
	0,11
	dull
	for textile and non-woven materials
	570
	24
	3,6-6,0
	1,0

	
	
	dope dyed black
	
	510
	27
	3,0 – 6,0
	2,0

	
	
	dull, “swan’s down” type
	for textile materials, as filler
	420
	40
	3,0 – 6,0
	2,0

	2
	0,12
	dull, “swan’s down” type
	for textile materials, as filler
	420
	40
	3,0 – 6,0
	2,0

	
	
	dull
	for artificial leather, textile materials
	420
	40
	3,0 – 6,0
	8,0

	
	
	dope dyed black
	
	
	48
	3,0 – 6,0
	2,0

	3
	0,13
	dull
	for textile and non-woven materials
	570
	24
	3,0 – 6,0
	1,0

	
	
	dope dyed black
	
	510
	27
	3,0 – 6,0
	2,0

	4
	0,15
	dull
	for textile and nonwoven materials
	540
	25
	3,0 – 6,0
	1,0

	5
	0,17
	dull
	for synthetic paper
	451
	56
	-
	2,0

	
	
	dull
	for textile and non-woven materials
	490
	35
	3,0-6,0
	1,0

	
	
	dull, “swan’s down” type
	for textile materials, as filler
	490
	35
	3,0-6,0
	1,0

	
	
	dope dyed black, “swan’s down” type
	
	480
	35
	3,0-6,0
	2,0

	
	
	dope dyed black
	for textile materials
	480
	34
	3,0-6,0
	2,0

	
	
	dull
	for processing in cotton and silk industries
	490
	33
	3,0-6,0
	1,0

	6
	0,22; 0,28
	dull
	for textile and non-woven materials
	400
	48
	3,0 – 6,0
	1,0

	
	
	dope dyed black
	
	
	
	3,0-6,0
	1,5

	7
	0,28; 0,33
	dull, “swan’s down” type
	for textile materials, as filler
	390
	50
	3,0 – 6,0
	2,0

	
	
	dope dyed black, “swan’s down” type
	
	370
	
	3,0-6,0
	

	8
	0,33; 0,44
	dull
	for textile and non-woven materials
	392
	50
	3,0 – 6,0
	2,0

	
	
	dope dyed black
	
	373
	
	
	

	9
	0,33; 0,44
	dull with increased elongation
	
	400
	50-70
	2,0 – 6,0
	5,0

	
	
	dope dyed black with increased elongation
	
	
	
	
	

	10
	0,6
	dull, “swan’s down” type
	for textile and non-woven materials, as filler
	370
	56
	3,0-6,0
	2,0

	
	
	dope dyed black, “swan‘s down” type
	
	350
	60
	
	3,0

	11
	0,6; 0,84
	dull
	for nonwoven ma-terials
	372
	58
	3,0-6,0
	2,0

	
	
	dope dyed black
	
	333
	60
	
	3,0

	12
	1,2; 1,7
	dull
	
	294
	70
	3,0-6,0
	3,0

	
	
	dope dyed black
	
	284
	70
	
	3,0

	13
	0,44
	dull, round hollow cross section, with “slippery handle”
	for yarns, nonwo-ven materials, as filler
	390
	50
	3,0-6,0
	2,0

	
	0,64
	
	
	370
	56
	
	2,0

	14
	0,84
	dull, round hollow cross section
	
	370
	56
	3,0-6,0
	2,0

	15
	1,7
	
	
	294
	70
	2,0-5,0
	3,0

	16
	0,6; 0,64; 0,68
	dull, trilobal (delta) hol-low cross section
	
	370
	56
	3,0-6,0
	2,0

	17
	0,44; 0,64
	dull, bicomponent fiber “core-sheath” type
	for thermobonded nonwoven materials
	240
	75
	1,5-6,0
	50


We have our own logistics department and can sell products on FCA, DAP and DDP basis. 
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