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Polyester Staple Fiber (100% Virgin)
(PTA base)
(HS Code 5503200000)
Hollow polyester fiber, “conjugate” type, siliconized and non-siliconized 0,78 tex, textile grade, to be used for nonwovens manufacturing and as a filling material.

Hollow polyester fiber, “conjugate” type, siliconized and non-siliconized 1,7 tex, textile grade, to be used for nonwovens manufacturing and as a filling material.

Dull polyester fiber, standard, 0,156 tex, textile grade, intended for manufacturing of textiles and nonwovens, including nonwoven materials type “spunlace”.

Dull polyester fiber, standard, 0,17 tex, textile grade, intended for manufacturing of textiles and nonwovens, including nonwoven materials type “spunlace”.

Dull polyester fiber, standard 0,33 tex, textile grade, intended for textiles and nonwovens manufacturing.

Physical and mechanical properties of the fiber:

	No.
	Description
	Nominal linear density of a filament, tex
	Nominal fiber length, mm
	Application
	Tenacity, mN/tex, not less than
	Elongation at break, %, not more than
	Shrinkage in hot air (180°С 15 minutes), %, not more than
	Number of crimps per 2,5 см/1см

	1
	Hollow polyester fiber, “conjugate” type, siliconized
	0,78
	32;38;66
	Fiberfill
	290
	55
	3,0
	4,0/-

	2
	Hollow polyester fiber, “conjugate” type, non-siliconized
	0,78
	32;38;66
	Nonwoven material production
	290
	55
	3,0
	4,0/-

	3
	Hollow polyester fiber, “conjugate” type, siliconized
	1,7
	32;38;66
	Fiberfill
	320
	50
	3,0
	5,0/-

	4
	Hollow polyester fiber, “conjugate” type, non-siliconized
	1,7
	32;38;66
	Nonwoven material production
	320
	50
	3,0
	5,0/-

	5
	Solid dull polyester fiber, standard type
	0,156
	32;38;66
	Textile and nonwovens production
	580
	25
	6,0
	-/4,0-7,0

	6
	Solid dull polyester fiber, standard type
	0,17
	32;38;66
	Textile and nonwovens production
	570
	28
	6,0
	-/4,0-7,0

	7
	Solid dull polyester fiber, standard type
	0,33
	32;38;66
	Textile and nonwovens production
	400
	40
	5,0
	-/4,0-7,0


We have our own logistics department and can sell products on FCA, DAP and DDP basis. 
tel. +375 222 49 9, 49 93 41; fax +375 222 76 40 11, 76 40 12
e-mail: market@khimvolokno.by                                                                       www.khimvolokno.by
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