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Polyethylene Terephthalate

textile grade

(HS Codes: 3907608000)

Polyethylene terephthalate grade D2 - for the manufacture of textile yarns, nonwovens and polyester fiber.

Physical and chemical properties of the polyethylene terephthalate:

	Parameter description
	Values

	Weight of 100 pellets, g
	4,0±0,5

	Specific viscosity in dichloroacetic acid, units
	833±7

	Titanium dioxide content, %
	0,30±0,02

	Moisture (water) content, % w/w, not more than
	0,1

	Color difference coordinates CIE 1976 with illuminant D65, geometry d/8°(d/10°) specular component excluded:
L*, units, not less than
b*, units, not more than
	
80
5

	Carboxyl end groups (carboxylic number), mmol/kg, not more than
	30

	Diethylene glycol content, % w/w, not more than
	1,1

	Softening (melting) point, °C
	259±2


Polyethylene terephthalate is packed in soft specialized containers for bulk products with polyethylene liners or in other containers, ensuring the safety of the product during transportation and storage.
The mass of polyethylene terephthalate in the container should be from 500 to 1050 kg (В± 3.0 kg. tolerance).
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 Polyethylene Terephthalate 
bottle grade
(HS Codes: 3907610000)

Polyethylene terephthalate 8200 type L
Application:

Polyethylene terephthalate 8200 is used for manufacture of disposable packing materials.
Physical and chemical properties:

	Parameter
	Value
РЕТ 8200 type L

	Appearance
	white granules

	Weight of 50 granules, g
	0,95-1,20

	Dust content, %, not more
	0.05

	Intrinsic viscosity in dichloroacetic
acid, dl/g
	0.78-0.82

	Acetaldehyde (АА) content, ррm, not more
	1,0

	Color difference CIELAB 1976, at D 65/10, specular component excluded:
- L units, not less than
- a* units
-b* units, not more
	


73.9
-1.4±1.5
0.8

	Moisture content, %, not more
	-


Packaging:

Polyethylene terephthalate 8200 type L is packed in special soft containers with PE liner for bulk products. Each container is mounted onto a wooden pallet.

Weight in a container – 1000,0 ±3,0 kg.
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